# Text boxes

Certificate No:

JUL-170403HESNZ

This is to certify that the nominated size and quality of the following TITAN product has been thoroughly inspected and tested, using the pre-determined load.

56T X 10MTR

56000KG

BLUE ROUNDSLING, ORANGE POLYESTER COVER

583.13kn

17/07/2017

ID NUMBER

Size / Length / Width

Color

Manufactured and tested for and on behalf of:

Testing Date

BATCH TEST RESULT

MBL

42 Clements Avenue

Bundoora Victoria 3083 Australia

Phone + 61 3 9466 7840

Fax: + 61 3 9466 7743

Description

Sling Material / Construction

TiTAN

LIFTING

TECHNOLOGIES

TOWING LINE

TEST CERTIFICATE

56T10-201707-001 TO 021

Polyester